- The RTP35T thick-film non-inductive power resistor, also known as a TO263-packaged high-power resistor, utilizes the TO263 package form—a common SMT surface-mount package type for high-power transistors, medium-to-small-scale integrated circuits, and power resistors.

- The RTP35T resistor is rated at 35W and features a bottom-mounted heat sink flange design for superior thermal dissipation. It is typically designed for current sensing, energy absorption and dissipation, RC snubbers, high-speed switching, and high-frequency transmission circuits. It is also commonly used in voltage regulation, constant power loads, and low-energy pulse loads. Applications span industries such as industrial lasers, welding equipment, test equipment, instrumentation, UPS systems, automotive, and switching power supplies.

TO263 Package RTP35T Thick-Film Resistor

Technical Specifications

| Rated Power | Insulation Resistance | Maximum voltage | Output terminal | Insulation Withstand Voltage |
| --- | --- | --- | --- | --- |
| 35W | ≥10GΩ | 500VDC | Tin-plated copper wire | 2000VAC |
| Resistance range | Operating Temperature | Optional precision | TC | Installation torque |
| 0.1Ω— | -55℃ | ±0.5% | ±100 | M3 maximum 0.9Nm |
| 1MΩ | +170℃ | ±5% | ppm/℃ |  |

| Test Item | Perf Req | Test Standard |
| --- | --- | --- |
| Overload | ΔR≤±0.25%R | 1.5P rated power not exceeding 1.5Umax, 5s |
| Lifetime | ΔR≤±1%R | 2000h at rated power Steady-State Humidity and Heat |
| Steady-state humid heat | ΔR≤±0.25%R | MIL-Std-202,Method 103, Condition D |
| Thermal shock | ΔR≤±0.3%R | -65 to 155°C, 5 cycles |
| High-frequency vibration | ΔR≤±0.2%R | MIL-Std-202, Method 204, Condition D |
| Lead strength | ΔR≤±0.2%R | MIL-Std-202, Method 211, Condition A |

Performance